## Slide 1: Bolted joints with radial pretension for thick-walled composites structures
Lutz Beyland, Composite Design Engineer,
German Aerospace Center (DLR) Institute of Composite Structures and Adaptive Systems
Elisabeth Ens
RWTH Aachen
ICCS20, International Conference on Composite Structures
4-7 September 2017 – CNAM, Paris, France

## Slide 2: Outline
State of the art bolted joints in thick walled laminates
Concept of bolted joint with radial pretension
Analytical approach
FE-Calculation
Bearing tests
Conclusion and Outlook

## Slide 3: Bolted joints for thick laminates - state of the art
Fields of application for many decades
  multi-stage rockets for transportation of satellites
  connection of aircraft wing and fuselage
  root connection of rotor blades of wind turbines
Failure modes
Tension
Shear Out
Cleavage
Bearing
Payload adapter Ariane 5 [DIEM]
T-Bolt connection for rotor blades [HAU]

## Slide 4: Problems of state of the art bolted joints
Joint stiffness and wear depend on bolt-hole clearance
Avoiding big bolt-hole clearance leads to
  High effort for precise drilling of borehole
  Need for reaming / drilling of both joint parts in one process
Big Clearance
P
P
Low Stiffness, high wear
P
P
High Stiffness, medium wear
Small / No Clearance
Radial Pretension
P
P
Very high stiffness, low wear

## Slide 5: Concept of radial pretension
Clamping bush overcomes clearance and creates a radial pretension between bolt and bore hole
Radial pretension by axial tightening of inner and outer ring
Outer ring of clamping bush is slatted >> Diameter increase of 1 mm possible
2 - No Clearance
3 - Radial Pretension
1 - Clearance
Inner ring
Outer
ring
Bolt
Plate with bore hole
Outer ring
Inner ring
Outer ring
Inner
ring
Clamping bush [MÄDLER]
Notes: Spannring = clamping ring
Ausführung = Implementation

## Slide 6: Research topics on bolted joint with radial pretension
Analytic model
to describe stress state around bore hole
FE model
to validate mathematical model and
for detailed analysis
Bearing tests
Static and fatigue strength

## Slide 7: Analytic approach
Pretension [Timoshenko]
Bolt load [Zhang]
Superposition
Notes: Quasiisotropic layoup
Disk under inner and outer pressure
Angle Theta

## Slide 8: 2D FE model - setup
FE-Software: Ansys Workbench 18.1
Boundary conditions
Symmetry at midplane
Fixed support of disk‘s peripheral surface
Bolt load as distributed force on bolt’s peripheral surface
Radial pretension by thermal expansion of bolt
Frictionless contact between bolt and hole
Material
Linear-elastic model
Disk: GFRP, quasi-isotropic stiffness
Bolt: Steel
Fixed
support
Bolt load
Thermal expansion
Disk
Bolt
Symmetry

## Slide 9: 2D FE model - results
Radial stress
Parameter | Variable | Value | Unit
Radius bore hole | a | 32,5 | mm
Outer radius disk | b | 800 | mm
Young‘s Modulus disk | E | 27 | GPa
Poisson's ratio disk | ν | 0,343 | -
Pretension | pi | 270 | MPa
Radial expansion (caused by pretension) | u0 | 0,5 | mm
Bolt load | p | 28 | kN/mm
Use case

## Slide 10: Comparison of analytical and FE model
Circum-
ferential path
Stresses at bore hole (circumferential path)
σrad maximum difference: 2 MPa
σtan maximum difference: 5 MPa
Conclusion: Analytical model is accurate for stresses at bolt hole

## Slide 11: Comparison of analytical and FE model
Radial path
Stresses at bore hole (radial path)
σrad maximum difference: 16 MPa (~7%)
σtan maximum difference: 20 MPa (~17%)
Conclusion: Analytical model is sufficient for stresses at whole disk

## Slide 12: Effect of friction on stress distribution – 2D-FE
Friction strongly influences stress distribution
Coefficient of friction µ between bolt and hole is not well known
Literature [Cuntze] suggests µ = 0,1 – 0,3
>>> µ = 0,1 chosen
Near
Sliding
Sticking
Contact status
µ = 0
µ = 0,1
µ = 0,5
Circum-
ferential path

## Slide 13: Effect of pretension on stress distribution – 2D-FE
Amount of pretension significantly influences both radial and tangential stress
High pretension avoids clearance under bolt load >> no tangential stress peak at
Medium pretension results in minimum overall tangential and radial stresses
Szenario | Pretension pi [MPa] | Expansion u0 [mm]
High pretension | 270 | 0,5
Medium pretension | 135 | 0,25
No pretension | 0 | 0
Circum-
ferential path

## Slide 14: Bearing test setup
Special 3-Point bearing test setup
Laminate thickness t = 10…20 mm
Maximum static load: F = 500 kN
Maximum fatigue load: -50 kN < F < +200 kN
Specimen GFRP
[+45 / -45 / 0 / 90]5s
Bolt
d = 40 mm
Bore hole for fixation
Bearing failure

## Slide 15: Clearance fit vs. radial pretension
Clearance fit
Clamping bush for radial pretension
Clearance = 0,1 mm
Radial expansion u0 = 0,4…0,8 mm

## Slide 16: Results in bearing strength
Bearing strength
  F… bolt load at failure
  d… hole diameter
  t… laminate thickness
Static bearing strength with radial pretension -15% compared to clearance fit
Fatigue bearing strength with radial pretension +40% compared to clearance fit
High pretension results in slightly higher fatigue strength

## Slide 17: Conclusion and Outlook
Conclusion
Analytic model for bolted joints with radial pretension is found and validated by FE-calculation (neglecting friction and cleavage)
Friction has a big impact especially on tangential stresses
Radial pretension results in smooth distribution of stresses around the bore hole
Bearing tests with radial pretension show an increase in fatigue strength, but a decrease in static strength
Outlook
Detailed understanding of bearing failure with radial pretension
Prediction of failure load from FE-calculation >>> failure criteria for bearing
Bearing tests with different pretensions >> evaluation of optimum pretension
Bearing tests with combined radial and axial pretension

## Slide 18: MANY THANKS FOR YOUR ATTENTION !
Lutz Beyland, Composite Design Engineer,
German Aerospace Center (DLR), Institute of Composite Structures and Adaptive Systems
Lilienthalplatz 7, 38108 Braunschweig, Germany
Lutz.Beyland@DLR.de
DO YOU HAVE ANY QUESTIONS ?

## Slide 19: References
[DIEM] Diem, H.: Tragfähigkeit von Bolzenverbindungen in dickwandigen Faserverbundstrukturen; Dissertation; TU München; 19.2.2007
[HAU] Hau, E.: Windkraftanlagen: Grundlagen, Technik, Einsatz, Wirtschaftlichkeit, Springer Berlin Heidelberg, ISBN 978-3-540-72150-5
[MÄDLER] Mädler GmbH: Spannsätze COM-AS Bohrung 19 bis 100mm; http://www.maedler.de/product/1643/1621/spannsaetze-com-as-bohrung-19-bis-100mm; accessed on 30.8.2017
[TIMOSHENKO] Timoshenko, S.: Theory of Elasticity; McGraw- Hill; 1934
[ZHANG] Zhang, K.-D.; Ueng, C. E.: Stresses Around a Pin-loaded Hole in Orthotropic Plates; Journal of Composite Materials 18 (1984), No. 5, p. 432-446
[CUNTZE] CUNTZE, R.; Das Versagensmoduskonzept, ein praktikables Auslegungswerkzeug bei neuen Leichtbauwerkstoffen“; Handout, Dresdner Leichtbausymposium, 7.-9. June 2001

## Slide 20: Anhang

## Slide 21: Lösungsraum für segmentierte Rotorblätter
JOULE III
Enercon
E126
Gamesa
Innoblade
Indeol / CENER
Modular
Wind Energy
JOULE III
Connection principle
Detachable
Non-Detachable
Bolting in longitudinal direction
Bolting in transversal direction
Bolting of pieces with a large overlap
Welding of thermoplasts
Bonding of thermosets
T-bolts
Metallic inserts
Form-fit
Force-fit
Connection tubes
Bolting of shear web
Single lap
Multi lap
Single lap
Multi lap
Megawind
JOULE III
DEBRA-25
T-bolts
Metallic inserts
Connection tubes
Multi lap

## Slide 22: Wo teilen?
0.2
1
0
0.3
0.4
0.5
0.6
0.7
0.8
Transportation
Extra mass = dynamic loads
Spar cap loads
Secondary loads
Big extra mass = extra cost
Little space
Bolting
Bonding

## Slide 23: Konzept „Stegverschraubung“
Schnitt A-A
Wurzel-
Gurte
Tip
Gurte
Wurzel-Steg
Tip-Steg
z
x
Schraube mit Mutter (ca. M36)
Stegbuchse Wurzelsegment
Stegbuchse Tipsegment
Stegbuchse Tipsegment
Stegbuchse Wurzelsegment
ca. 5m
Detail Z
y
x
Wurzel-Gurt
Wurzel-Stege
Tip-Stege
Tip-Gurt
y
x
Schnitt B-B
z
y
Detail Z
A
A
B
B

## Slide 24: CAD-Modell „Stegverschraubung“ in Nordex-Rotorblatt NR58.5
tipseitige Verschraubung
wurzelseitige
Verschraubung

## Slide 25: Segmentiertes Rotorblatt – Testpyramide (10-2016)
Coupon-Tests
Lochleibungstests
Biegebalken
Full
Scale
Test
Bauteil-Tests Verschraubte Holme
Design
Konzeptentwicklung
Vorauslegung
CAD-Modellierung

## Slide 26: Lochleibungstests BiLo
Klebstoff
>> verklebte Probe ohne Flansch
Spannbuchse
>> verspannte Probe
>> gesteckte Probe
Spielpassung

## Slide 27: Rax-Buchse – Funktionsdemonstrator + Patentanmeldung