## Slide 1: Lightweight Design: The Vanguard of Automotive Engineering Strategies for Materials and Construction Methods
Prof. Dr.-Ing. Horst E. Friedrich
Dipl.-Ing. Gundolf Kopp
Dipl.-Ing. Marco Münster

## Slide 2
Agenda
1. Growing importance of lightweight construction
2. Methodical approach in the development process
3. Lightweight construction strategies
4. Challenge: lightweight construction in the volume segment
5. Concepts for current and future cars
6. Trends in materials and structures yesterday, today and tomorrow

## Slide 3
We are reaching the limits of oil extraction
Climate change is taking place
Growing population, concentrated in big cities and conurbations
Demographic trend
Lower energy consumption
Reduced CO2 emissions
Alternative and regenerative energy sources
Automated driving / connectivity
…
Source: DLR
Source: versust.blogsport
Source: http://www.fotocommunity.de/pc/pc/mypics/1438338/display/18369424
Vehicle concepts
Megatrends

## Slide 4: CO2 emissions in new vehicles in Germany and EU CO2 limits
Source: KBA; DLR
* Mass-dependent

## Slide 5: Total of normal resistances and consumption
FL
Differential consumption factors for 100 kg weight reduction in a vehicle with spark-ignition engine
FSt
FR
FB
FL
FSt
FR
FB
Normal resistances
Source: DLR; Rohde-Brandenburger, Volkswagen AG
Chart: 
| NEFZ | i angepasst NEFZ | vh angepasst NEFZ
Verbrauch für 100 kg / (l/100 km) | 0.15 | 0.32 | 0.39
Consumption per 100 kg/ (l/100 km)
urban
combined
highway
0,15
0,32
0,39
i adjust NEFZ
vh adjust NEFZ

## Slide 6
28 %
Source: DLR
Increase in range [%]
Mass reduction [%]
25 %
Extension of range with small electric vehicles
Artemis Urban (with recuperation)
Artemis Urban (without recuperation)
NEFZ (with recuperation)
NEFZ (without recuperation)

## Slide 7
- Running resistances
Lateral dynamics dependent on CG (SP)
- Unsprung mass
- Secondary effects
- Position of battery  Roll behavior
- Wheel hub drive  Yaw behavior
Lightweight design measures required
Influence of lightweight construction on vehicle dynamics
Opportunity for electromobility
Lightweight construction, vehicle dynamics and electromobility
Source: IVK Stuttgart, DLR
- Crosswinds
- Road transverse gradient
- Ruts, stochastic
unevenness
- More sensitive to
weight
conventional vehicle (ICE)
battery electric vehicle (BEV) or fuel cell vehicle (FCV)
battery or fuel cell tank
Notes: Logitudinal motions
Lateral motions

## Slide 8
Battery electric
vehicle
Hybrid electric
vehicle
Range extended electric
vehicle
CO2 reduction potential (g/km)
95
128
133
333
57
50
50
45
37
Cost of CO2 reduction (EUR/g)
Hybrid structures
(aluminum, magnesium, plastics)
Weight reduction of 420 kg
Battery electric
vehicle
Hybrid electric
vehicle
Range extended electric
vehicle
High strength steel
Weight reduction of 250 kg
Carbon fiber structures
Weight reduction of 490 kg
18
CO2 reduction cost and potential
(Example: medium sized car with 140 g CO2/km)
CO2 emissions in the production of materials
(kg CO2 eq./kg raw material)
Steel
13
24
31
31
140
50
84
36
ICE efficiency
Electric powertrain
Lightweight
Range
Source: McKinsey, Ecoinvent, EEA, DLR
Potential to minimize CO2 emissions
CFRP

## Slide 9
Demand for mobility
- CO2
- Legislation
- Energy prices
- …
- Requirements
- Target function
- …
Transport system
Vehicle concepts and architecture
Technology
- Simulation
- Optimization
- …
- Structural components
- Crash components
- Energy converters
- …
From the chain of effects of the traffic system to the methodical development process
Quelle: DLR

## Slide 10
Lightweight shape
Lightweight materials
Objective:
light vehicle with high crash performance (L7e)
Solution:
Body structure in sandwich architecture
  Skin layers aluminum alloy
  Foam core polyurethane
Joining process
  Crash-stable structural adhesive
  Welded parts
Euro-NCAP frontal crash  intrusion approx. 102 mm
Lightweight concept
Lightweight
requirement
Source: DLR
BIW < approx. 80 kg
Lightweight requirement

## Slide 11
Lightweight shape
Lightweight materials
Lightweight
requirement
Objective:
- Crash modular, adaptable vehicle front
- Three-dimensional, reinforced light
front vehicle structure
Energy absorbed through cutting
Approx. 20% lighter than steel reference structure
„weak“
„medium“
„strong“
Source: DLR
Solution:
Lightweight design concept
- Peeling pipes for adjustment of energy
Lightweight concept

## Slide 12
Objective:
- Light CFRP B-pillar
Solution:
Layer structure (0/90/45)
Manufacture using VARI procedure
Internal reinforcement with additional Omega profile
Lightweight material design
Source: DLR
Lightweight shape
Lightweight concept
Lightweight
requirement
Lightweight materials

## Slide 13
Objective:
- BIW weight reduction ≥ 85 kg (≥ 30%)
- Lightweight construction costs (cost of parts) ≤ 5 €/kg
Solution:
Body in white 100 kg lighter than reference (approx. 35%)
Complete CAD model of the BIW
Validation of structure (crash, static etc.)
Specification of joining and production processes
Life cycle analysis for MMD concept
Lightweight material design
Materials
Percent by weight
Aluminium 96kg (53%)
Steel 66 kg (36%)
Magnesium 11 kg (7%)
Plastics 7 kg (4%)
Aluminium sheet
Aluminium cast
Aluminium extrusion
Steel
Hot-formed steel
Magnesium sheet
Magnesium diecasting
Glasfibre thermoplastic
Source: VW, DLR
Lightweight shape
Lightweight concept
Lightweight
requirement
Lightweight materials

## Slide 14
Solution:
New design with magnesium alloy
Integration of suspension strut slot and A-pillar
Weight saving approx. 50 %
Objective:
A-pillar cast node lighter and more cost-attractive
Lightweight shape
Source: DLR
Lightweight shape
Lightweight concept
Lightweight
requirement
Lightweight materials

## Slide 15
Lightweight construction potential
Series size
FRP-
intensive
- CFRP; GFRP
Light metal-
Intensive
- Al; Mg
Steel-intensive
- ductile; high-strength and
highest-strength steel
Multi-
Material-
Design
Adjusting lever for lightweight construction:
  Materials
  Concepts
  Production technology
  etc.
  …
  Weight
  Safety
  NVH
  etc.
t
Challenge: lightweight construction in the volume segment
Source: VW; Daimler; DLR

## Slide 16
Weight saving:
  structural weight reduced by about 100 kg
    Electrics - 6 kg
    Drive train - 40 kg
    Chassis - 26 kg
    Body - 37 kg
Lightweight design measures:
  High-strength and higher-strength types of steel, reduced sheet thickness (TRB)
  Only using material where it is needed
  Optimal geometry of profiles and surfaces
Chart: 
 | 0.2 | 0.11 | 0.32 | 0.09 | 0.28
28%
32%
20%
11%
9%
Mild Steel
High-Strength Steel
Highest-Strength Steel
Advanced-High-Strength Steel
Ultra-High-Strength Steel, hot formed
Concept: steel-intensive Example: Golf VII
Source: VW

## Slide 17
Source: ATZ; www.carsuk.net
Weight saving:
  Vehicle about 420 kg lighter than its predecessor
  Weight saved in basic shell approx. 39% (almost 180 kg)
Lightweight design measures:
  External skin panels between 0.9 and 1.5 mm
  All body joints riveted or bonded
  Side parts compressed in a single aluminum component
   Fewer body joints
  High-strength Al AC300 for the crash structure
Concept: Aluminum-intensive Example: Range Rover V

## Slide 18
Concept: Aluminum-/steel-intensive hybrid design
Example: Audi TT 2nd generation
Weight saving:
  Weight of body: 206 kg
  Reference body in steel would be 48% heavier
  Pure Al body would be 12% lighter
Lightweight design measures :
  Multi-material-desgin
  Shell and space frame structure combined
Aluminum 69%
  Sheet metal 63 kg
  Cast components 45 kg
  Extruded profiles 32 kg
Sheet 31%
  Sheet metal 66 kg
Source: Audi

## Slide 19
CFRP "Life" module
Aluminum “Drive" module
Source: www.bimmertoday.de
Source: www.bimmertoday.de
Weight saving:
  Vehicle total weight approx. 1195 kg with battery
  Approx. 300 kg saved through new material and purpose-built design
Lightweight design measures:
  Material combination CFC + aluminum
  Bi-modular design
    "Life" module - CFC monocoque body
    "Drive" module - crash and structural components, Al chassis
Source: BMW
Concept: Bi-module (CFRP-Al-intensive) Example: BMW i3

## Slide 20
Concept: CFRP-intensive Example: F125!
Correctly use the good material characteristics of Steel, Aluminum, Composites
strain/ tensile strength
Energy absorption
Thickness
S
A
A
S
S
A
C
C
CFC
CFC sandwich
Metal-plastic hybrid
Weight saving:
  CFRP-intensive design approx. 250 kg lighter than current reference
  Front curved and support structures designed as load-bearing assembly unit in CFRP sandwich hybrid design
Lightweight design measures:
  Ultra-light fiber composite body
  Structure-integrated hydrogen storage
  Function integration through CFRP e.g. safety belt integrated into seat structure
Source: Daimler

## Slide 21: Trends in materials & structures yesterday, today
Skeleton/
Space Frame
Monocoque
Shell construction
Space Frame/
frame structure
Audi A8
Al Space Frame
Lamborghini Aventador
CFRP- monocoque
BMW M6
St- Shell + AL & CFRP
Mercesdes-Benz W196
frame structure
Steel
Light metal
FRP
Source: Audi; VW; Daimler

## Slide 22: Trends in materials & structures yesterday,today,tomorrow
Skeleton/
Space Frame
Monocoque
Shell construction
Space Frame /
frame structure
Steel
Light metal
FRP
Bi-modular
Desgin
Hybrid
Desgin
Audi A8
Al Space Frame
Lamborghini Aventador
CFRP- Monocoque
BMW M6
St- Shell + AL & CFRP
Mercesdes-Benz W196
frame structure
?
Source: Audi; VW; Daimler

## Slide 23
Summary
CO2 limits are driving forward lightweight construction in vehicle design
Gradual electrification is reinforcing the trend towards lightweight construction
  Compensation for extra weight of new components
Further development of construction methods:
  Increase in MMD in volume-intensive production sector
Focus for research and development:
  Consideration overall, methodical approach in the product development process
Source: DLR
Vehicle concepts and lightweight design
Materials and processes
Methods and simulation

## Slide 24: Thank you for your attention!